Anchor Scan Parameters

Dataset Name:	SAMPEL ST
File name:	D:\SEMEN PADAN NOVEMBER\27 DESEMBER 2018\RIZKI\SAMPEL ST\SAMPEL ST.XRDML
Sample Identification:	15.unp
Comment:	Configuration=factory_settings, Owner=ADM, Modification date=2016-01-27 07:36:46
	Goniometer=PW3050/60 (Theta/Theta), Minimum step size 2Theta=.005, Minimum step size Omega=.005
	Sample stage=Spinner PW3805
	Diffractometer system=CubiX3
	Scan program=UNP__Marett_2017, Owner=ADM, Modification date=12/26/2018 1:58:58 PM
Measurement Date / Time:	12/26/2018 1:59:44 PM
Operator:	Unknown
Raw Data Origin:	XRD measurement (*.XRDML)
Scan Axis:	Gonio
Start Position [°2Th.]:	10.0100
End Position [°2Th.]:	100.0100
Step Size [°2Th.]:	0.0200
Scan Step Time [s]:	10.1600
Scan Type:	Continuous
PSD Mode:	Scanning
PSD Length [°2Th.]:	2.55
Offset [°2Th.]:	0.0000
Divergence Slit Type:	Fixed
Divergence Slit Size [°]:	0.9570
Specimen Length [mm]:	10.00
Measurement Temperature [°C]:	25.00
Anode Material:	Cu
K-Alpha1 [Å]:	1.54060
K-Alpha2 [Å]:	1.54443
K-Beta [Å]:	1.39225
K-A2 / K-A1 Ratio:	0.50000
Generator Settings:	30 mA, 40 kV
Diffractometer Type:	3550
Diffractometer Number:	0
Goniometer Radius [mm]:	200.00
Dist. Focus-Diverg. Slit [mm]:	91.00
Incident Beam Monochromator:	No
Spinning:	Yes

Graphics

Peak List

Pos.[°2Th.]  Height [cts]  FWHMLeft[°2Th.]  d-spacing [Å]  Rel. Int. [%]
    34.4446         70.03           0.3936        2.60382          63.32  
    37.8762         86.08           0.3936        2.37543          77.84  
    41.5711         83.17           0.3149        2.17244          75.20  
    44.3342        110.59           0.3936        2.04325         100.00  
    45.9221         88.71           0.4723        1.97623          80.22  
    46.9012         91.34           0.3149        1.93723          82.59  
    55.8557         42.06           0.4723        1.64604          38.03  
    62.7781         51.62           0.4723        1.48016          46.67  
    82.1278         71.77           0.4723        1.17360          64.90  

Pattern List

Visible  Ref.Code     Score    Compound Name         Displ.[°2Th]  Scale Fac.  Chem. Formula         
         01-085-1410       17  Iron                         0.000       0.677  Fe                    
         01-088-0315        1  Iron Oxide                   0.000       0.617  Fe3 O4                
         01-079-0007        0  Iron Oxide                   0.000       1.024  Fe2 O3                
         00-003-0812        1  Iron Oxide                   0.000       0.648  Fe2 O3                
         00-003-0800  No Matc  Iron Oxide                   0.000       0.000  Fe2 O3                

Document History

Insert Measurement:
- File name = "SAMPEL ST.XRDML"
- Modification time = "12/28/2018 7:58:59 AM"
- Modification editor = "User"

Default properties:
- Sample name = ""
- Sample prepared by = ""
- Measurement step axis = "None"
- Sample mode = "Reflection"
- Internal wavelengths used from anode material: Copper (Cu)
- Original K-Alpha1 wavelength = "1.54060"
- Used K-Alpha1 wavelength = "1.54060"
- Original K-Alpha2 wavelength = "1.54443"
- Used K-Alpha2 wavelength = "1.54443"
- Original K-Beta wavelength = "1.39225"
- Used K-Beta wavelength = "1.39225"
- Dist. focus to div. slit = "91.00000"
- Irradiated length = "10.00000"
- Receiving slit size = "0.10000"
- Step axis value = "0.00000"
- Offset = "0.00000"
- Sample length = "10.00000"
- Modification time = "12/28/2018 7:58:59 AM"
- Modification editor = "User"

Interpolate Step Size:
- Derived = "Yes"
- Step Size = "0.01"
- Modification time = "12/28/2018 7:58:59 AM"
- Modification editor = "PANalytical"

Smooth:
- Polynomial type = "Quintic"
- Convolution range = "25"
- Degree of smoothing = "18"
- Fast Fourier = "Yes"
- Omit Peaks = "Yes"
- Modification time = "12/27/2018 1:32:15 PM"
- Modification editor = "User"

Search Peaks:
- Minimum significance = "1"
- Minimum tip width = "0.3"
- Maximum tip width = "1"
- Peak base width = "2"
- Method = "Minimum 2nd derivative"
- Modification time = "9/25/2018 2:45:15 PM"
- Modification editor = "User"

Search & Match:
- Allow pattern shift = "No"
- Auto residue = "Yes"
- Data source = "Profile and peak list"
- Demote unmatched strong = "No"
- Multi phase = "Yes"
- Restriction set = "Untitled"
- Restriction = "Restriction set"
- Subset name = ""
- Match intensity = "Yes"
- Two theta shift = "0"
- Identify = "No"
- Max. no. of accepted patterns = "5"
- Minimum score = "25"
- Min. new lines / total lines = "50"
- Search depth = "10"
- Minimum new lines = "3"
- Minimum scale factor = "0.0001"
- Intensity threshold = "0"
- Use line clustering = "Yes"
- Line cluster range = "1.5"
- Search sensitivity = "1.8"
- Use adaptive smoothing = "Yes"
- Smoothing range = "1.5"
- Threshold factor = "3"
- Modification time = "5/26/2015 8:52:30 AM"
- Modification editor = "User"

Search & Match:
- Allow pattern shift = "No"
- Auto residue = "Yes"
- Data source = "Profile and peak list"
- Demote unmatched strong = "No"
- Multi phase = "Yes"
- Restriction set = "Untitled"
- Restriction = "Restriction set"
- Subset name = ""
- Match intensity = "Yes"
- Two theta shift = "0"
- Identify = "No"
- Max. no. of accepted patterns = "5"
- Minimum score = "25"
- Min. new lines / total lines = "50"
- Search depth = "10"
- Minimum new lines = "3"
- Minimum scale factor = "0.0001"
- Intensity threshold = "0"
- Use line clustering = "Yes"
- Line cluster range = "1.5"
- Search sensitivity = "1.8"
- Use adaptive smoothing = "Yes"
- Smoothing range = "1.5"
- Threshold factor = "3"
- Modification time = "5/26/2015 8:52:30 AM"
- Modification editor = "User"

Search & Match:
- Allow pattern shift = "No"
- Auto residue = "Yes"
- Data source = "Profile and peak list"
- Demote unmatched strong = "No"
- Multi phase = "Yes"
- Restriction set = "Untitled"
- Restriction = "Restriction set"
- Subset name = ""
- Match intensity = "Yes"
- Two theta shift = "0"
- Identify = "No"
- Max. no. of accepted patterns = "5"
- Minimum score = "25"
- Min. new lines / total lines = "50"
- Search depth = "10"
- Minimum new lines = "3"
- Minimum scale factor = "0.0001"
- Intensity threshold = "0"
- Use line clustering = "Yes"
- Line cluster range = "1.5"
- Search sensitivity = "1.8"
- Use adaptive smoothing = "Yes"
- Smoothing range = "1.5"
- Threshold factor = "3"
- Modification time = "5/26/2015 8:52:30 AM"
- Modification editor = "User"